## Slide 1
Lattice energy of ionic crystals
Ionic crystals is considered as 3D arrays of point charges. The forces that held them together is electrostatic and can Be calculated by adding all the electrostatic repulsion and attractions.
The Lattice energy (U) is the net potential energy of the arrangement of charges that forms the crystal structure
This lattice energy is equivalent to the energy need to sublime the crystal (i.e. into gaseous ions)
The value of U depends on the crystal structure, the charge on the ions and the internuclear separation between anions and cations.
Two principal kinds of force determine ionic crystal structures
(a) Electrostatic forces of attraction and repulsion
The attractive force F is given by
Consider two ions MZ+ and XZ− separated by a distance r

## Slide 2
The coulomb potential energy is given by
(b) Short range repulsive force (when ions are very close)
B a constant and n = 5 to 12
The lattice energy is calculated by combining the net electrostatic attraction and the Born repulsion energies
and finding the internuclear separation, re, which gives the maximum U value.
Consider the NaCl structure. . Between each pair of ions there is an electrostatic
interaction
For each Na+, there are 6 nearest neighbors (Cl--)
Next nearest neighbors (12 Na+ ions) at edge centres
third nearest neighbors (8 Cl-) ions) at cube corners

## Slide 3
The net attractive energy between our Na+ ion and all other ions in the crystal is given by
This summation is repeated for each ion in the crystal, i.e. for 2N ions per mole of NaCl. Since each ion pair interaction is counted twice, it is necessary to divide the final value by 2
Where A is the Madelung constant (summation of the numerical
values
The Madelung constant depends only on the geometric arrangement of the point charges

## Slide 4
The total energy of the crystal is given by
differentiating with respect to r to find the maximum U value and
equilibrium interatomic distance, re
Lattice energy as a function of internuclear separation
Born-Lande equation

## Slide 5
Born-Haber Cycle
The lattice energy of a crystal is equivalent to its heat of formation from 1 mol of its ionic constituents in the
gas phase
Na+(g) + Cl- (g) → NaCl(s), H = U
This can not be measured experimentally. However, the heat of formation of a crystal, Hf , can be measured
relative to the reagents in their standard states
Na(s) + 1/2Cl2(g) → NaCl(s),  H =  Hf
Hf may be related to U by constructing a thermochemical cycle known as a Born–Haber cycle,
Na(s) → Na(g)  Hatm
Cl2(g) → 2Cl(g)  Hdis
Na(g) → Na+(g)  Hion
Cl(g) → Cl-(g)  HEA
The unknown lattice enthalpy can be calculated by summing up all the enthalpy changes. Sum of enthalpy changes round a complete cycle is zero.
 Hf =  Hatm  Hdis +  Hion  HEA + U
Na+(g) + Cl- (g) → NaCl(s), H = U

## Slide 6
Born-Haber Cycle
Lattice energies (KJ/mol) of group I halides

## Slide 7
Crystal defects
In a perfect crystal, all the atoms are at rest on their correct lattice positions. Such a perfect crystal can be
obtained, hypothetically, only at absolute zero;
At all real temperatures, crystals are imperfect.
Crystals are invariably imperfect because the presence of defects up to a certain concentration leads to a
reduction of free energy.
Consider a perfect crystal with a single defect (vacant cation site). Creation of defects requires some amount energy H, but increases the entropy, S.
This is due to the large number of positions this defect can occupy. For 1 mol of cations there will be 1023 possible positions.
According to Boltzmann equation
S = k.ln W
W is the probability
The energy needed to create a defect is more then compensated by the increase in the entropy.

## Slide 8
G =  H − T  S
However, at higher defect concentration (>10%) the entropy contribution is small as the crystal is already disordered. Further, the energy required to create more defects will be higher.
Types of defects
Defects are broadly divided into two types
Stoichiometric defects (intrinsic defects)
Where the composition of the crystals is unchanged
Non-Stoichiometric defects (extrinsic defects)
Change in composition of the crystals is observed
Defects are classified depending on their size and shape.
Point defect :involves one atom/site (vacancies)
Line defect: dislocations
Plane defect: Whole layer of the crystal can be defective

## Slide 9
Point defects: Schottky and Frenkel
cation
anion
Interstitial cation
Schottky
Frenkel
Equal numbers to anion and cation vacancies will be formed to maintain electroneutrality.
The charge of the cation vacancy is -1 it is +1 for anion vacancy.
Eg: NaCl
Eg: AgCl
The interstitial Ag is in 8 co-ordination. Some covalent interaction is possible resulting in stability
This is observed in high CN crystals
In some cases the ions will move from Tb to Oh sites. Thus, these defects are noted in low coordination structures

## Slide 10
Anti-exchange or anti-site
This type of defect is common in metal alloys with exchange of neutral atoms where pair of ions are interchange their positions.
This is an unfavorable arrangement. It is noted at high temperatures.
Extrinsic defects
This is resulted from doping of impurity atoms to the crystals.
Cr:Al2O3
Ti:Al2O3
Naturally occurring gemstones are with impurities. They possess trap states for electrons.
Doping of d-metal is the origin of color of the gemstones
Dopants cause vacancies
Ca2+ doping in ZrO2 results in
oxygen vacancies

## Slide 11
Color centers
When alkali halides like NaCl, KCl are heated in the vapor of alkali metal produces color.
F-centers (Farbenzcentre)
For example, uptake of Na in NaCl gives nonstoichiometric Na1+δCl where δ is very much lea than 1, which has a greenish yellow colour
The Na atoms ionize at the crystals surface and the resulting Na+ ions reside at the surface but the electrons diffuse inside the crystal and occupy vacant anion sites.
To preserve charge balance, an equal number of Cl− ions must find their way out to the surface.
The trapped electron provides a classic example of an ‘electron in a box’. A series of energy levels are available for the electron within this box and the energy required to transfer from one level to another falls in the visible part of the electromagnetic spectrum; hence the colour of the F-centre.
The magnitude of the energy level and color depends on the host crystals and not on the way the defect is produced.

## Slide 12
F-centres can be created by irradiation. For example, bombardment of NaCl with X-rays produces color due to trapped electrons. Which are released due to ionization of Cl- ions.

## Slide 13
Solid Solutions
A solid solution is basically a crystalline phase that can have variable composition.
If the dopant concentration is > 1% it is appropriate to consider them as solid solutions
In a solid solution, there can be more than two components. The one which is in higher concentration is called base metal or solvent and the other component is called an alloying element or solute.
In a solid solution, the solute components reside on the lattice structure of the base metal.
Depending on the location of the solute element, the solid solutions are divided into 2 categories
Substitutional solid solutions
Interstitial solid solutions
Where, the atom or ion that is being introduced replaces an atom of the base metal and occupies their lattice sites
Substitutional solid solutions
Example: Cr-Al2O3 ((Al2−xCrx)O3: (0 ≤ x ≤ 2)
Ni atoms are replaced by Cu

## Slide 14
Solid Solutions
The substitutional solid solution can be further classified depending on the order of replacement of base metal by the solute.
Ordered substitutional solid solutions
Random or disordered substitutional solid solutions
In ordered substitutional solid solutions, the solute atoms which replace base metal occupy the lattice in an ordered fashion.
In disordered substitutional solid solutions, the solute atoms occupy random location of the base metal resulting in a disordered arrangement.
Interstitial solid solutions
Where, the newly doped species i.e. the solute atoms occupy the interstitial sites or the empty spaces of the base metal.
As the size of the empty space is limited in the crystal, the interstitial solid are generally formed by atoms (solute) with small sizes.
If the solute is a d-block metal, the probability to form interstitial solid solution is high due to their small ionic radii as well as due to their electronic structure.

## Slide 15
Metals form interstitial solid solutions in which small atoms, especially H, C, B and N, enter empty interstitial sites within the host metal structure.
Eg: PdHx: 0 ≤ x ≤ 0.7 ; tungsten carbide
The small atoms preserve the crystal structure and there will be no electron transfer
Examples: Alloys formed from metals with similar size and charge, NiCu ; ZnCu
In some cases, an interstitial alloy may be regarded as a substitutional alloy derived from another lattice.
Carbon steels: C atoms occupy some of the octahedral holes in the -Fe fcc lattice.

## Slide 16
Hume-Rothary rules
Hume-Rothary formulated few rules which governs the formation of substitutional solid solutions.
1. Crystal Structure
For good solid solubility the two elements should possess same crystal structure.
The solute and the solvent (base metal) should be of similar size. The difference in the radii must be within 15% for the solid solution to form without distortion.
2. Size factor
3. Chemical affinity factor
The difference in electronegativity between the solute (alloying metal) and the base metal must be small. Generally, elements which are near to each other in the periodic table possess small EN difference.
4. Charge
The ions which replace each other must have same charge. If not, structural changes might occur (vacancies) to maintain charge neutrality.

## Slide 17
Solid Solutions
Effect of temperature
Increase in temperature favours solid solution formation.
1. Increase in Entropy
2. Enthalpy if negative, then solid solution formation is favoured at all higher temperatures
Enthalpy if negative, then solid solution formation is likely at higher temperatures
Intermediate solid solution
Addition of excess (solid solubility) of alloy metal into the base metal, may result in a second new phase
This second phase may possess different crystal structure and properties from solid solutions
These phases are intermediate between solid solution and compounds

## Slide 18
Aliovalent solid solutions
Where the charge of the host metal is different from the charge of the solute (alloying) metal
This causes changes in the crystal lattice which are compensated by (a) ionic compensation and (b) electronic compensation
ionic compensation
electronic compensation
Na1−2xCaxVxCl

## Slide 19
Na1−2xCaxVxCl : small amount of CaCl2 is mixed in NaCl lattice
Creating cation vacancies
Creating interstitial anions
Ca1−xYxF2+x: small amount of CaF2 is mixed in YF3 lattice
Creating anion vacancies
Zr1−xCaxO2−x: 0.1 < x < 0.2
Quartz: Lix(Si1−xAlx)O2: 0 < x ≤ 0.5 where Si4+ is replaced with Al3+
Creating interstitial cations
Cation vacancies may be generated by deintercalation
Electronic compensation
Eg. Removal of Li+ (and an electron) from LiCoO2 .
Holes are created for the charge balance and forms Li1−xCo1−x3+Cox4+ O2

## Slide 20
Elements and stoichiometry: Individual groups, Metals, non-metals, and metalloids, Allotropes of carbon, phosphorus, and other elements, Binding Energies. why stoichiometry is important (4 Lecture)
Basic redox chemistry- recapitulation of balancing equations, oxidation number, various electrochemical cells (viz. Daniel cell, concentration cells), electrolysis cells and electroplating, Nernst Equation, reduction potential, standard electrodes (viz. silver, calomel, hydrogen), Factors affecting reduction potential, pH electrode, corrosion as redox reaction, few examples of redox processes in biological systems, Latimer diagram, Pourbaix diagram, Cyclic voltammetry basics: half-cell potential, triangular wave scan, Ficks law, Randles-Sevick equation interpretation, basic application (8 lectures)
Introduction to solids: Amorphous vs. crystalline solids, types of crystalline solids, Bravais lattice, crystal systems, unit cell, close packing of various types, packing density, examples of close packed structures, radius -ratio, ionic solids, Madelung constant, Born-Lande equation, basic thermodynamics of ionic crystal (viz. Born-Haber cycle), discrepancies in lattice energy, calculations of void spaces and packing parameters, point defects (Schottky and Frenkel), colour centres and their influence, metals and their packing, influence of impurities on metals, utility of alloys, Hume-Rothary rules, basics of doping and conductivity, Miller Indices-concept of planes, indexing planes, symmetry and equivalent planes. (10 lectures)
Books for reference:
1. Inorganic chemistry By Catherine E Housecroft and Alan G. Sharpe
2. Inorganic Chemistry By Shrivers Atkins And Langford
3. Solid State Chemistry and its applications by Anthony R West
Syllabus